# A practice-based handling evaluation of 3M ESPE Filtek Silorane

Evaluation date: January 2008

Summary: The positive reception of this novel material is indicated by the 67% of evaluators who would purchase the Filtek Silorane system & that 73% would recommend the system to colleagues.

Published: Dental Practice 2010; February: 28-30

F.J Trevor Burke, DDS, MSc, MDS, MGDS FDS (RCS Edin.), FDS RCS (Eng.), FFGDP(UK), FADM

Russell J Crisp, BDS, DGDP

Primary Dental Care Research Group,

## University of Birmingham School of Dentistry

St. Chad’s Queensway

Birmingham B4 6NN, UK

Voice: 0044 121 237 2767

Fax: 0044 121 237 2768

Email f.j.t.burke@bham.ac.uk

INTRODUCTION

Practice-based research

The importance of practice-based research has been emphasized by Mandel, who considered that “research is not only the silent partner in dental practice, it is the very scaffolding on which we build and sustain a practice”1. In this respect, a wide variety of research projects may be considered to be appropriate to general dental practice.  These include2:

- Assessment of materials and techniques

- Clinical trials of materials

- Assessment of treatment trends and treatment of disease

- Assessment of behaviour and attitudes (of dentists as well as patients)

- Evaluation of disease incidence

- Patient satisfaction

The volume of clinical material seen in general dental practice makes dental practice an area of fundamental importance in the assessment of new techniques and materials, as success of a material, device or technique could be considered to be its performance in everyday use in a particular dentist’s office. Central to good performance of dental materials are, not only, their physical properties, but also their ease of use, given that it could be suggested that a device or restorative which handles easily will be more likely to produce an optimally performing restoration than one which is difficult to use. The assessment of the handling of a new material, or a revised version of an older one, is therefore of importance.

The performance or handling of a restorative material by one operator is necessarily subjective, but when practitioners band together to form a group in order to assess the handling of new materials in dental practice, the results are likely to be more objective and generalisable. All of this is possible when practitioner-based research groups are teamed with the expertise available in academic institutions.  A UK-based group of practice-based researchers is the PREP (Product Research and Evaluation by Practitioners) Panel. This group was established in 1993 with 6 general dental practitioners, and has grown to contain 28 dental practitioners located across the UK and 3 in mainland Europe. It has completed almost 60 projects –  “handling” evaluations of materials & techniques, and more recently, clinical evaluations (n=8) of between 1 year and 5 years.

Resin composite restorations

Since the ability to bond to enamel was first described by Buonocore in 19553  this has become an integral part of restorative dentistry alongside the development of resin composite materials, with these materials becoming increasingly used worldwide4.  The majority of these materials shrink up to 3% on polymerisation, resulting in stresses at the (bonded) restoration margin, or within the restorative material itself. The magnitude of these stresses also depends on the modulus of elasticity of the material, the coefficient of thermal expansion, the bonding of the filler particles to the resin and their nature, and the configuration of the cavity into which the restoration is placed. It is obvious that one solution involved the use of a low shrink resin, and, ideally, that shrinkage should be balanced by the uptake of a similar %volume of moisture and the resultant expansion in the mouth.   The first material to fulfil these characteristics is 3M ESPE Filtek Silorane, which has a polymerisation contraction of 1%5.

Given the novel nature of this new material, it would seem appropriate  that  an assessment of its handling in the hands of general dental practitioners is carried out.  This study will therefore evaluate the in-practice ease of use and performance of Filtek SiloraneTM (3M ESPE, St.Paul, MN, USA) by the group of UK-based general dental practitioners who comprise the PREP Panel.

###### Materials and methods

The product under evaluation , Filtek™Silorane, is a low-shrink (<1% volumetric shrinkage tested by bonded-disc method) posterior composite restorative material (3M ESPE, Espe Platz, 82229 Seefeld, Germany.	Contact details:  3M ESPE Customer Service UK Tel. 01509 613121 and see also www.3MESPE.com).

Fifteen members of the PREP panel were selected at random to conduct the evaluation, of which two evaluators were female. The average time since graduation was 22 years, with a range of 8 to 32 years. Packs of the new material (in 4 shades) were sent to these15 practitioners in December 2007 with a request that they use the material, where indicated, for 10 weeks. They were also sent a questionnaire which was designed to evaluate their current posterior composite usage, and the presentation, instructions, handling, aesthetic quality and post-operative sensitivity of the new composite. Most responses to the questionnaire were given on a visual analogue scale.

### RESULTS

# Background information

All the evaluators (100%) normally placed composite restorations in posterior teeth, and the number of posterior composite restorations being placed by them in a typical week was as follows:

Number of restorations			No of respondents

<5						2 (13%)

5-10                                                          8 (53%)

>10						5 (33%)

Of these, the mean proportions of restorations placed were: Class I 40%, Class II 37%, and MOD restorations made up 23%.

When the evaluators were asked about techniques used the results were as follows:

a) Dentine bonding agent					13 evaluators

b) Glass-ionomer base/sandwich				6 evaluators

c) Flowable composite base layer + bonding agent 	11 evaluators

d) Other							1 evaluator

A wide range of posterior composite materials were used by the respondents prior to the evaluation, with four respondents using more than one material. The principal reasons for the choice of these materials were good aesthetics, ease of use, wear resistance, good results and familiarity. Other reasons reported were good results in clinical trials, trusted manufacturer, & compatability with a favoured bonding system. Fourteen (93%) of the evaluators used their present material in compule form.

When the evaluators were asked to rate the ease of use of their current posterior composite material, the result was as follow:

Difficult to use 1						              5    Easy to use

3.9

When the evaluators were asked to rate the ease of use of their current dentine/bonding system, the result was as follow:

Difficult to use 1						              5    Easy to use

4.6

The evaluators were asked to rate the aesthetic quality of restorations placed in posterior teeth using their current composite material with the following result:

Poor           1						                           5    Excellent

4.3

When the evaluators were asked how many different shades and opacities they used for one posterior restoration, on average, the result was 2 Shades and 1 opacity. 87% (n=13) of the evaluators stated that the current composite used for posterior restorations had sufficient number of shades, with a mean number of shades provided being 8 (range: 1 – 20).

A third (n= 5) of the evaluators stated that they knew the percentage shrinkage of the composite currently used and the mean value provided was 2.4%. A composite with minimal shrinkage was stated by all of evaluators to be an advantage. Reasons stated for this were:

- “Reduced post-operative sensitivity (10),

- “Less cuspal stress” (9 evaluators),

- “Reduced microleakage” (7),

- “Less stress on bonding agents” (4), and,

- “Better box adaptation” (1).

### Evaluation of Filtek Silorane

Evaluators rated the presentation of the kit as follows:

Poor         1						                            5    Excellent

4.0

When the evaluators were asked to rate the illustrated technique guide/instructions for Filtek Supreme, the result was as follows:

Poor         1						                            5    Excellent

4.7

The total number of restorations placed during the evaluation was 266, comprised of: Class 1 - 47%, Class - II 35%, and MOD - 18%.

When the evaluators were asked if they were satisfied with the Filtek Silorane System (ie Silorane + the Silorane adhesive system) 67% (n= 10) stated that they were.

Fourteen (93%) of the evaluators stated they had encountered no post-operative sensitivity with Filtek Silorane. The remaining evaluator encountered sensitivity in 2 of his 25 cases, making a total for the evaluation of 2 from 266 restorations, or 0.7% overall.

Overall 87% (n=13) of the evaluators stated they were satisfied with the Filtek Silorane restorative.

The ease of use of the Filtek Silorane restorative was rated by the evaluators as follows:

Difficult to use  1						               5    Easy to use

4.0

Twelve (80%) of the evaluators stated that the viscosity of Filtek Silorane was satisfactory and when they were asked to rate the viscosity of the material the result was as follows:

Not viscous    1						                5 Too viscous  enough

3.5

All the evaluators stated that the material had sufficient working time in clinical use. One evaluator stated that the material started to “dry up” in his headlight so he turned it off.

80% (n=12) of the evaluators stated that the restorations were easily finished using their normal polishing system, though three commented:  “Harder to achieve ‘gloss’ finish” and one evaluator stated it “took longer”.

The overall aesthetic quality of restorations of Filtek Silorane was assessed as follows:

Poor         1						                            5    Excellent

3.7

Nine of the evaluators (60%) thought the number of shades provided was adequate, with the following comments from those evaluators who wanted more shades: “Lighter shades needed” (2), “Less opaque shades” (2), and “I use a layered system but Filtek Silorane acceptable”.

When the evaluators were asked if the restorations of Filtek Silorane slumped prior to curing, all the evaluators stated that they maintained their shape.

If the Filtek Silorane system was available at an average price, 67% (n=10) of the evaluators stated that they would purchase the system. Comments from those who would not included: “Carefully used, my current system gives no post-operative sensitivity and superior aesthetics” and “Advantages of nil shrink outweighed by disadvantages”

73% (n=11) of the evaluators stated they would recommend the Filtek Silorane system to colleagues. Further comments included:

- “Excellent material & easier to condense than my regular composite”,

- “Tips of compules too big” (4 evaluators),

- “Poor aesthetics” (2 evaluators),

- “This is the best performing/handling composite I’ve used.

- “Sculptability is superb.

- “Ease of placement & speed excellent.

- “Minimal finishing needed”,

- “Good viscosity – packed well” (2)

All (100%) of the evaluators were satisfied with the adhesive system.

All (100%) of the evaluators stated that the Self-etch Primer was easy to apply and twelve (86%) stated that the Self-etch bond was also easy to apply. The viscosity of the bonding agent was rated as follows:

Not viscous    1						                5 Too viscous  enough                                                           3.7

One evaluator commented “ Bond bottle needs a redesign – like a Heinz ketchup or Hellmans mayonnaise bottle - so that it can stand on its top so adhesive ready at the end of the bottle”.(Figure 1)

The evaluators rated the ease of use of the Silorane System adhesive as follows:

Difficult to use  1						               5    Easy to use

4.0

Comments regarding the Silorane System Adhesive (Self-etch Primer & Bond) included “Excellent but cannot use for other composites”.

Discussion

The Filtek Silorane system has been subjected to an extensive evaluation in clinical practice by members of the PREP panel in which 266 restorations were placed. The presentation of the kit scored well in terms of the completeness of the components and their arrangement, ability to be placed on the working area and the overall presentation (all 4.0, or more, on a visual analogue scale where 5 = excellent and 1 = poor). The illustrated technique guide and the instructions were given a particularly high rating of 4.7 (on the visual analogue scale where 5 = excellent and 1 = poor).

A restoration in Filtek Silorane is presented in Figure2. In this respect, the overall aesthetic quality of restorations in Filtek Silorane was rated 3.7 (on a visual analogue scale where 5 = excellent and 1 = poor). This compared with 4.3 for the posterior composite material used prior to this evaluation, which was on average, provided in 8 shades. However, Filtek Silorane, being intended as a material for use in posterior teeth, has only four shades, which is likely to be the reason for any less than complimentary comments regarding the aesthetics of the material.

When rated for ease of use, Filtek Silorane scored 4.0 (on a visual analogue scale where 1 = difficult to use and 5 = easy to use) which was a near identical score for the previously used posterior composite material and the score of 3.5 (on a visual analogue scale where 5 = too viscous and 1 = not viscous enough) is close to the ideal median score. Overall, 87% of the evaluators stated that they were satisfied with the Filtek Silorane restorative, although four (27%) evaluators stated that the tips of the compules were too large. This is due to the material being of near “packable” consistency.

All the evaluators stated that they were satisfied with the Silorane system adhesive though one evaluator suggested an inverted design for the bond bottle to ensure easier dispensing (Figure 1).

CONCLUSIONS

The positive reception of this novel material is indicated by the 67% of evaluators who would purchase the Filtek Silorane system and that 73% of the evaluators would recommend the system to colleagues.

MANUFACTURER’S COMMENTS

3M ESPE would like to express their thanks to the members of the PREP panel for their thorough evaluation of Filtek Silorane Restorative System.

This and other studies have laid the foundations for the clinical success of this highly innovative and brand new restorative technology. The Filtek Silorane Restorative and Adhesive System offers handling characteristics and outstanding performance that will certainly influence the practitioners’ decision in making this their material of choice for posterior restorations. The majority of the PREP panel dentists would both purchase and recommend Fitlek Silorane to their colleagues. This is very good news for us. With the introduction of Filtek Silorane to the dental world, we are happy to be able to provide a material that sets new standards in low shrink chemistry and  technology, a reduction on the stress imposed on the restored tooth, and attractive handling characteristics that should appeal to dental professionals the world over.

ACKNOWLEDGMENT

The help of the members of the PREP Panel is greatly appreciated, as too is the funding of this project from 3M ESPE, Seefeld, Germany.

REFERENCES

1.Mandel ID.  Clinical research – the silent partner in dental practice.  Quintessence Int.1993:24:453-463.

2.Burke FJT, McCord JF.  Research in dental practice – problems and solutions.  Br.Dent.J.1993:175:396-398.

3.Buonocore MG A simple method of increasing the adhesion of acryl filling materials to enamel surfaces. J.Dent.Res.1955:34:849-853.

4. Burke F.J.T. Amalgam to tooth-coloured materials – implications for clinical practice and  dental education: governmental restrictions and amalgam-usage survey results. J.Dent.2004:32:343-350.

5.Filtek Silorane Product Profile, 2007, 3M ESPE

FIGURES

Figure 1. Suggested method for storing Silorane bond (courtesy of Frank Dolan, Glasgow).

Figure 2a. Amalgam restoration, leaking at distal gingival margin. (Illustration published by courtesy of George Warman Publications, publishers of Dental Update)

Figure 2b. Restoration in Figure 1 replaced by Filtek Silorane (IIlustration published by courtesy of George Warman Publications, publishers of Dental Update)